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NBS SPECIFICATION
K32 Panel Cubicles / MR MFC
Ascent Range Toilet Cubicle System
	PROJECT
[Insert project name]
	PREPARED FOR
[Architect / Contractor]
	DATE
October 2026
	REVISION / STATUS
A — For Approval


112   CUBICLE SYSTEM
	Location
	Refer to Architect's drawings.

	Manufacturer
	Bridgewater Direct, Unit 1C Britannia Business Park, Union Road, Bolton BL2 2HP. Tel: 0161 703 3980 · sales@bridgewaterdirect.co.uk · www.bridgewaterdirect.co.uk

	Product reference
	Ascent Range Toilet Cubicles — MR MFC cubicle system for damp and humid washrooms

	Panels
	18 mm moisture-resistant melamine faced chipboard (MR MFC), decorative finish both faces, to BS EN 14322.

	Panel thickness
	18 mm doors, pilasters and partitions.

	Edge treatment
	Square edge, with matching 2 mm ABS edging to all exposed edges.

	Overall height
	1950 mm, with 150 mm floor clearance (1800 mm panels).

	Partition depth
	1500 mm standard. Made to measure, 1400–1800 mm.

	Width & layout
	800–1200 mm per cubicle, 1–6 per run. Between walls, left or right corner, or freestanding.

	Doors
	Overlap the pilasters by 20 mm each side. Inward or outward opening, left or right hand hung. Outward opening doors 50 mm shorter to clear the headrail.

	Supports
	Adjustable cylindrical legs: one per partition, two per middle pilaster 300 mm wide or over.

	Headrail
	D-shaped aluminium headrail with end caps. Top aluminium channel available instead.

	Fittings & ironmongery
	Satin anodised aluminium (SAA) throughout: heavy-duty hinges, indicator latch and bolt, channel brackets and coat hook.

	Panel colour / finish
	To be confirmed by Architect. Full decor range and samples available on request.


250   INSTALLATION
1. Programming: Do not install cubicles or duct wall panels until the building is weathertight, wet trades have completed their work, wall and floor finishes are complete and the building is dried out.
1. Modifications: Do not cut, plane or sand prefinished components.
1. Fixing: Secure components using fasteners and methods recommended by the cubicle manufacturer, to prevent bowing or other distortion of frames, panels and doors.
1. Moisture and movement: Make adequate allowance for future movement.
SAMPLES & TECHNICAL SUPPORT
Decor samples, datasheets and project advice are available direct from Bridgewater Direct: call 0161 703 3980 or email sales@bridgewaterdirect.co.uk quoting the product reference above, or configure online at www.bridgewaterdirect.co.uk.
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