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NBS SPECIFICATION
K32 Panel Cubicles / Duct & Wall Linings / Screens
Ascent Range Vanity Unit System
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A — For Approval


130   VANITY UNITS — PANEL SYSTEMS
	Location
	Refer to Architect's drawings.

	Manufacturer
	Bridgewater Direct, Unit 1C Britannia Business Park, Union Road, Bolton BL2 2HP. Tel: 0161 703 3980 · sales@bridgewaterdirect.co.uk · www.bridgewaterdirect.co.uk

	Product reference
	Ascent Range Vanity Units — MR MFC vanity unit system for damp and humid washrooms

	Panels
	18 mm moisture-resistant melamine faced chipboard (MR MFC), decorative finish both faces, to BS EN 14322.

	Panel thickness
	18 mm

	Edge treatment
	Square edge, with matching 2 mm ABS edging to all exposed edges.

	Worktop height
	850 mm adult, 650 mm junior or 550 mm infant, floor to worktop surface.

	Depth
	600 mm (fully recessed basins) or 400 mm (semi-recessed). Made to measure, 250–700 mm.

	Width & layout
	1–6 basins per run, made to measure. Between walls, corner, freestanding or L‑shaped.

	Upstand & downstand
	100 mm upstand and 200 mm downstand, factory fitted.

	Access panels
	Removable front access panels, supplied loose to fit after the plumbing is tested.

	End panels
	Exposed ends in decorative finish; ends against walls in service finish.

	Alternative top
	White solid surface trough with a tap hole and plug to each basin, optional 100 mm plant-on upstand. For units 600 mm deep or over.

	Panel colour / finish
	To be confirmed by Architect. Full decor range and samples available on request.


250   INSTALLATION
1. Programming: Do not install vanity units until the building is weathertight, wet trades have completed their work, wall and floor finishes are complete and the building is dried out.
1. Modifications: Do not cut, plane or sand prefinished components. Basin and tap openings are cut on site: seal all cut edges. Basins, taps and wastes by others.
1. Fixing: Secure units to a solid background or studwork using fasteners and methods recommended by the manufacturer, to prevent bowing or other distortion of carcass, worktop and panels.
1. Moisture and movement: Make adequate allowance for future movement.
SAMPLES & TECHNICAL SUPPORT
Decor samples, datasheets and project advice are available direct from Bridgewater Direct: call 0161 703 3980 or email sales@bridgewaterdirect.co.uk quoting the product reference above, or configure online at www.bridgewaterdirect.co.uk.
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